GI 00200

EARTHWORK FOR GREEN INFRASTRUCTURE PROJECTS

GI 00200.01 Description.

Excavate soils for bioretention facilities, pervious surfaces, and other green infrastructure installations in a manner that does not compact subgrade or reduce infiltration capacity of subgrade. Work also includes placement of backfill and filter materials.

GI 00200.02 Applicable Standards.

- City of New Orleans Department of Public Works General Specifications for Street Paving (Current Standards)

NO DPW C130: MATERIALS, EQUIPMENT, EMPLOYEES, CONTRACTOR QUALITY CONTROL

NO DPW C203: PREPARATION OF ROADWAY PAVEMENT SUBGRADE

Sewerage and Water Board of New Orleans General Specifications (Current Standards)

- NO S&WB 073: REINFORCED CONCRETE PIPE FOR DRAINS

NO S&WB 080: EXTRA STRENGTH REINFORCED CONCRETE PIPE FOR DRAINS

- GI 00126:	Site Activity for Green Infrastructure Projects

- GI 01003:	Aggregate for Green Infrastructure Projects

- GI 00605:	Pervious Concrete Pavers

- GI 00606:  Precast Porous Concrete Panels

GI 00200.03 Submittals.

Contractor shall submit to the project Designer at the preconstruction meeting the following information:

As part of GI 00126 - Site Activity Plan, contractor shall provide a description of the equipment and methods used to excavate the green infrastructure facility and backfill with specified materials in a manner that does not overly compact the subgrade or backfill materials. For the purposes of this Special Provision, a green infrastructure facility is any area that is designed to capture, retain, and/or temporarily detain the runoff to the existing conveyance system. This includes but is not limited to bioretention facilities and pervious paving systems.

GI 00200.04 Summary of Work.

- General

- Furnish all labor, materials, equipment and incidentals required and perform all excavation work and grading; place and compact backfill and fill; and dispose of unsuitable, waste and surplus materials.

Earthwork associates with areas outside of the green infrastructure facility shall be in accordance with the respective Section NO DPW C203, NO S&WB 073, NO S&WB 080, etc. or as otherwise indicated on the drawings.

- Excavation

- Excavations for green infrastructure facilities are to be protected from heavy equipment that would result in compaction of soils within the footprint, unless compaction is specified in the construction documents. All excavation areas designated for green infrastructure facilities shall be field marked prior to commencing excavation.

Furnish, install, monitor and maintain excavation support (e.g., shoring, sheeting, bracing, trench boxes, etc.) as required by Federal, State or local laws, ordinances, regulations and safety requirements. Support the sides of excavation, to prevent any movement which could in any way reduce the width of the excavation below that necessary for proper construction and protect adjacent structures from undermining, settlement or other damage. Take care to prevent the formation of voids outside of sheeting. If voids occur behind sheeting, immediately backfill and compact the voids with common fill material. Voids in locations that cannot be properly compacted upon backfilling shall be filled with lean concrete.

Excavation supports shall be carefully removed in such manner so as not to endanger the Work or other adjacent structures, utilities, property, or green infrastructure facilities. All voids left or caused by withdrawal of supports shall be immediately filled with sand and compacted. Excavation supports may remain in place if approved by the City.

Contractor shall be solely responsible for determining the means and methods for meeting the requirements of excavation of the materials to prevent compaction of the soils within the green infrastructure facility footprint including side slopes. Utilize low ground-contact pressure equipment on green infrastructure facilities to minimize compaction. Low ground-contact pressure equipment includes equipment with wide or high-flotation tires (34 to 72 inches wide), dual tires, equipment with bogey systems, or tracked machinery. No heavy equipment shall be used within the perimeter of the facility before, during, or after excavation and installation of materials. Use of equipment with narrow tracks or narrow tires, rubber tires with large lugs, or high pressure tires will cause excessive compaction resulting in reduced infiltration rates and shall not be allowed by the project Designer.

All areas that have been adversely compacted during construction shall be alleviated using a primary tilling operation such as a chisel plow, ripper, or sub-soiler. These tilling operations are to re-fracture the soil profile through the 12-inch compaction zone. Substitute methods for re-fracturing must approved by the project Designer.

Excavation within 1-foot of final grade shall not be permitted if the project site soil is frozen or has been subjected to greater than 0.25-inches of precipitation within the previous 48 hours, or unless otherwise approved by the project Designer.

Excavated sides and bottom of green infrastructure facility shall be scarified 2-3 inches with the teeth of an excavator or other tools to promote infiltration.

- Prepare Subgrade

- Verify as-constructed or existing subgrade elevation and perform additional grading operations as necessary to bring the subgrade to a true slope parallel to the finished grade, at all areas to receive soil mixes.

Any subgrades or soils polluted by gasoline, oil, plaster, construction debris, unacceptable soils, or other substances which would render material unsuitable for plant growth, shall be removed from the premises whether or not such pollution occurred or existed prior to or during the Contract period. In the event that such material is placed, this material shall be removed and replaced with approved material. All remedial operations associated with soil mixes shall be reviewed and approved by the project Designer.

Clean subgrade and dispose of all debris prior to placement of aggregates and soil mixes.

Remove all large clods, lumps, brush, roots, stumps, litter, trash, and other foreign material and stones one-half inch in diameter or larger.

Mechanically or hand remove all vegetation on subgrade.

Protect adjacent pavements, walls, utilities and other construction from damage or staining by any backfill, aggregate, and soil mix placement operations.

- Compaction Requirements

- Do not compact under green infrastructure facilities unless specifically required per the Designer and Construction Documents.

General subgrade compaction, outside of green infrastructure facility footprint and side slopes shall be per NO DPW C203 and GI 00126.

- Geotextiles

- Geotextiles shall comply with GI 00206 – GEOSYNTHETICS FOR GREEN INFRASTRUCTURE FACILITIES.

Geotextile fabric shall be placed in the footprint of the green infrastructure facility to the limits shown on the Drawings.

Geotextile fabric shall be placed according to the requirements of NO DPW C203.07. All other materials shall be placed according to the requirements in this specification and the contract documents.

- General Filling and Backfilling Procedures

- The underdrain, aggregate, geotextile, and/or soil materials shall not be installed until contributing drainage areas are stabilized to the satisfaction of the Designer. Any discharge of sediment that affects the performance of the green infrastructure facility shall be corrected to restore hydraulic performance.

- Fill and backfill materials shall be placed in lifts to suit the lines and grades required, making allowances for settlement and placement of cover materials (i.e. soil, mulch, etc.)

- Fill and backfill materials for GI facilities shall not be placed on frozen surfaces, or surface covered by snow or ice unless otherwise approved by the project Designer. Fill and backfill material shall be free of snow, ice, and frozen earth.

- Fill and backfill shall not be placed and compacted when the materials are too wet to properly compact (i.e., the in-place moisture content of the soil at that time is no more than three percentages points above the optimum moisture content of that soil as determined by the laboratory test of the moisture-density relation appropriate to the specified level of compaction).

- Clay Barriers and Berm Material and Placement

- Clay barriers and/or berms between adjacent green infrastructure facilities and other areas, if designated shall be constructed USCS Soil Classification of CH, CL, or MH and have permeability no less than 1 x 10-7 cm/sec.

- Field compaction to 95% standard maximum density per ASTM D-1557.

- Underdrain/Observation Wells/Cleanouts

- Underdrain pipes shall be installed as directed in the contract documents.

- Material of underdrains and cleanouts shall be PVC or HDPE meeting the requirements of GI 00704, unless otherwise noted on the Drawings.

- Grading

- Grading shall be performed to the lines and grades shown on the Drawings. All objectionable material encountered within the limits indicated shall be removed and disposed. Subgrades shall be completely and continuously drained and dewatered throughout the grading process.

- If at the time of grading, it is not possible to place any material in its proper section of the work, it shall be stockpiled in approved areas for later use. No extra payment will be made for the stockpiling or double handling of excavated material.

- All cut and fill slopes shall be uniformly dressed to the slope, cross-section, and alignment shown on the Drawings.

Access, Sequencing, and Scheduling: The contractor shall notify the Designer at key times of operation to allow for materials/site observations. Failure to notify the Designer could result in the rejection of material and/or work. Provide 24 hour advance notice of performing the following tasks:

- Completion of excavation

- Installation of underdrain and/or cleanouts

- Placement of aggregate

- Placement of bioretention soil

- Placement of plants

- Placement of mulch

GI 00200.05 Measurement.

- The basis of payment for earthwork associated with a green infrastructure facility footprint and side slopes, excluding earthwork paid for in other items, shall be measured by the cubic yard, theoretical section, computed by the average end area methods. This shall encompass all labor, materials, overhead, and profit.

- Unsuitable subgrade, excavation, and sand filling, where directed by the Designer, shall be measured by the cubic yard truck measure. This shall encompass all labor, materials, overhead, and profit.

- The method of measurement and basis for payment for earthwork associated with pervious paving facilities shall be in accordance with the measurement and payment requirements contained in GI 0078, GI 0605, GI0606, NO DPW C506, and NO DPW C604.

- All other items associated with green infrastructure earthwork shall be measured as indicated in other applicable specification sections.

GI 00200.06 Payment.

Payment for excavation will be made at the contract unit prices. Payment will be made under:

| ITEM NO. | PAY ITEM | PAY UNIT |
| --- | --- | --- |
| GI-0200-01-A | Open Space Excavation for GI Facilities | CY |
| GI-0200-01-B | Right-of-Way Excavation for GI Facilities | CY |
| GI-0200-02 | Unsuitable Subgrade, Excavation, & Sand Filling | CY |