GI 00206

GEOSYNTHETICS FOR GREEN INFRASTRUCTURE FACILITIES

GI 00206.01 Description.

The Contractor shall furnish all labor, materials, equipment and incidentals required to install geosynthetic materials as required in the Contract Documents.

GI 00206.02 Applicable Specifications

City of New Orleans Department of Public Works General Specifications for Street Paving (Current Standards)

- NO DPW C201:	CLEARING AND GRUBBING

- NO DPW C202:	REMOVAL OF STRUCTURES AND OBSTRUCTIONS

- NO DPW C203:	PREPARATION OF ROADWAY PAVEMENT SUBGRADE

- NO DPW C204:	ENVIRONMENTAL PROTECTION AND STORMWATER

- POLLUTION PREVENTION PLAN

- NO DPW C719:	LANDSCAPING

- NO DPW C723:	GRANULAR MATERIAL

LA DOTD Standard Specifications for Roads and Bridges (Current Standards)

- LA DOTD 203:		EARTHWORK AND SITE PREPARATION, TEMPORARY

- EROSION CONTROL

- LA DOTD 701:		INCIDENTAL CONSTRUCTION, CULVERTS AND STORM

- DRAINS

- LA DOTD 702:		INCIDENTAL CONSTRUCTION, MANHOLES, JUNCTION

- BOXES, CATCH BASINS, AND END TREATMENTS

- LA DOTD 711:		INCIDENTAL CONSTRUCTION, RIPRAP

- LA DOTD 712:		INCIDENTAL CONSTRUCTION, REVETMENTS

- LA DOTD 726:		INCIDENTAL CONSTRUCTION, BEDDING MATERIAL

- LA DOTD 1018:	MATERIALS, MISCELLANEOUS MATERIALS

- LA DOTD 1019:	MATERIALS, GEOTEXTILE FABRIC AND GEOCOMPOSITE SYSTEMS

GI 00126: 		SITE ACTIVITY PLAN FOR GI PROJECTS

GI 00200: 		EARTHWORK FOR GI PROJECTS

GI 00204:		EROSION & SEDIMENTATION CONTROL FOR GI FACILITIES

GI 00605:		PERVIOUS PAVERS

GI 00606:		PRECAST POROUS CONCRETE PANELS

GI 01003: 		AGGREGATES FOR GI FACILITIES

GI 01005: 		BIORETENTION SOILS FOR GI FACILITIES

GI 00206.03 Applicable Standards

- American Society for Testing and Materials (ASTM):

| D123 | Standard Terminology Relating to Textiles |
| --- | --- |
| D276 | Standard Test Methods for Identification of Fibers in Textiles |
| D751 | Standard Test Methods for Coated Fabrics |
| D792 | Standard Test Methods for Density and Specific Gravity (Relative Density) of Plastics by Displacement |
| D882 | Geotextile Class 1 shall meet the requirements of AASHTO M 288. |
| D1004 | Standard Test Method for Tear Resistance (Graves Tear) of Plastic Film and Sheeting |
| D1203 | Standard Test Methods for Volatile Loss from Plastics Using Activated Carbon Methods |
| D1204 | Standard Test Method for Linear Dimensional Changes of Nonrigid Thermoplastic Sheeting or Film at Elevated Temperature |
| D1239 | Standard Test Method for Resistance of Plastic Films to Extraction by Chemicals |
| D1790 | Standard Test Method for Brittleness Temperature of Plastic Sheeting by Impact |
| D4354 | Standard Practice for Sampling of Geosynthetics and Rolled Erosion Control Products (RECP) for Testing |
| D4355 | Standard Test Method for Deterioration of Geotextiles by Exposure to Light, Moisture, and Heat in a Xenon Arc Type Apparatus |
| D4439 | Standard Terminology for Geosynthetics |
| D4491 | Standard Test Methods for Water Permeability of Geotextiles by Permittivity. |
| D4533 | Standard Test Method for Trapezoid Tearing Strength of Geotextiles. |
| D4595 | Standard Test Method for Tensile Properties of Geotextiles by the Wide Width Strip Method |
| D4632 | Standard Test Method for Grab Breaking Land and Elongation of Geotextiles. |
| D4751 | Standard Test Method for Determining Apparent Opening Size of a Geotextile |
| D5199 | Standard Test Method for Measuring the Nominal Thickness of Geosynthetics. |
| D5261 | Standard Test Method for Mass Per Unit Area (Weight) of Woven Fabric. |
| D6241 | Standard Test Method for Static Puncture Strength of Geotextiles and Geotextile Related Products Using a 50-mm Probe |
| D6637 | Standard Test Method for determining Tensile Properties by the single or Multi-Rib Tensile Method |
| D7176 | Standard Specification for Non-Reinforced Polyvinyl Chloride (PVC) Geomembranes Used in Buried Applications |
| D7748 | Standard Method for Flexural Rigidity of Geogrids, Geotextiles, and Related Products |

GI 00206.04 Submittals.

Contractor shall submit to the project Designer product data for each geosynthetic:

- Product identification and manufacturer name

List of material properties

GI 00206.05 Quality Assurance

- Use only material that has been approved by the Design Professional.

Use adequate numbers of skilled workmen who are thoroughly trained and experienced in the necessary crafts and who are completely familiar with the specified requirements and the methods needed for proper performance of the work of this section.

Field Demonstration

Demonstrate field connections for review and approval prior to proceeding with installation.

Demonstrate field connections are secure and function as desired. Fasteners or connectors, except for geotextile seams, are not subject to strength tests, but are required to hold geosynthetic panels together during installation and fill placement.

Field Quality Control

- Maintain quality control documentation. Include information on geosynthetic placement and alignment control. Submit daily copies to the Field Representative. Update files at the end of each work week and check to assure all pertinent information is included in each file.

Discard damaged geosynthetics. No repairs will be allowed.

Place all backfill, cover material and compact in such a manner to ensure geosynthetics remain undamaged.

GI 00206.06 Definitions.

- Cross-Machine Direction - the direction in the plane of the fabric perpendicular to the direction of manufacture. (ASTM D4632)

Machine Direction - the direction in the plane of the fabric parallel to the direction of manufacture. (ASTM D4632)

MARV - Minimum average roll value.

Ultraviolet (UV) Resistance - the deterioration in tensile strength from exposure to ultraviolet light generally expressed as percent strength retained for a certain length of exposure.

Geotextile – a permeable geosynthetic comprised solely of textiles (ASTM D4439)

Permittivity – the volumetric flow rate of water per unit cross sectional area per unit head under laminar flow conditions, in the normal direction through a geotextile (ASTM D4491).

GI 00206.07 Delivery, Storage, and Handling.

During shipment and storage, the geosynthetic shall be wrapped in a heavy-duty covering to protect it from direct sunlight, ultraviolet rays, temperatures greater than 140 degrees F. (60 degrees C.) mud, dirt, dust, debris and abrasion.

The Contractor shall check the geosynthetic, upon delivery, to assure the proper material has been received.

Special care shall be taken in the handling of geosynthetics manufactured from polypropylene when temperatures are at or below 0 degrees F (-18 degrees C).

Deliver, store, and handle geosynthetic materials in accordance with manufacturer's recommendations and as specified herein. When manufacturer's recommendations and requirements of this specification conflict use the more stringent method of delivery, storage, and handling.

- Store geosynthetics to prevent exposure to ultraviolet radiation.

Elevate geosynthetics above ground to protect from standing and flowing water.

Cover geosynthetics to prevent rainwater from infiltrating and saturating the materials.

Do not drive or operate mechanical equipment directly on geosynthetics.

Materials delivered to the project site without identification will be rejected.

Field mark similar materials (i.e., if two types of geotextiles are used) for quick identification.

GI 00206.08 Materials.

The following are the characteristics and properties of geosynthetics if unspecified in the plans:

- Subsurface Drainage Applications:

- Geosynthetics shall meet the requirements of AASHTO M 288.

- Class 2 geosynthetics may be used for all applications unless otherwise noted on the Drawings, by the Owner, or by the Designer.

  - Class 1: A geosynthetic fabric for use in applications where there is a high risk of damage during construction due to construction equipment or dumped aggregates.

| Property | Test Method | Unit | Specification Limit |
| --- | --- | --- | --- |
| Elongation | ASTM D4632 | % | <50 |
| Grab Strength |  | N (minimum) | 1400 |
| Tear Strength | ASTM D4533 | N (minimum) | 500 |
| Puncture Strength | ASTM D6241 | N (minimum) | 2750 |
| Permittivity | ASTM D4491 | Sec-1 | 0.1 |
| Apparent Opening Size | ASTM D4751 | mm | 0.22 |
| UV Stability (at 500 hours) | ASTM D4355 | % strength retained (minimum) | 50 |

  - Class 2: A geosynthetic fabric for use in applications where there is little to average risk of damage during construction due to construction equipment or dumped aggregates.

| Property | Test Method | Unit | Specification Limit |
| --- | --- | --- | --- |
| Elongation | ASTM D4632 | % | <50 |
| Grab Strength |  | N (minimum) | 534 |
| Tear Strength | ASTM D4533 | N (minimum) | 223 |
| Puncture Strength | ASTM D6241 | N (minimum) | 1380 |
| Permittivity | ASTM D4491 | Sec-1 | 7.7 |
| Apparent Opening Size | ASTM D4751 | mm | 0.212 |
| UV Stability (at 500 hours) | ASTM D4355 | % strength retained (minimum) | 70 |

Pervious Paving Applications. Geosynthetic Class 2 shall meet the requirements of AASHTO M 288.

| Property | Test Method | Unit | Specification Limit |
| --- | --- | --- | --- |
| Elongation | ASTM D4632 | % | <50 |
| Grab Strength |  | N (minimum) | 534 |
| Tear Strength | ASTM D4533 | N (minimum) | 223 |
| Puncture Strength | ASTM D6241 | N (minimum) | 1380 |
| Permittivity | ASTM D4491 | Sec-1 | 7.7 |
| Apparent Opening Size | ASTM D4751 | mm | 0.212 |
| UV Stability (at 500 hours) | ASTM D4355 | % strength retained (minimum) | 70 |

Impermeable Membrane. Material that is used to prevent infiltration and contain stormwater within the facility by lining the sides and bottom.

- Shall have a thickness of 30 mil and confirm to the following requirements:

| Property | Test Method | Unit | Specification Limit |
| --- | --- | --- | --- |
| Thickness | ASTM D5199 |  | +/- 5% |
| Specific Gravity | ASTM D792 | (Minimum) | 1.20 |
| 100% Modulus | ASTM D882 | psi (minimum) | 1000 |
|  |  | Lb force/in width (min) | 30 |
| Tensile |  | psi (minimum) | 2300 |
|  |  | Lb force/in width (min) | 73 |
| Elongation Break |  | % (minimum) | 380 |
| Graves Tear | ASTM D1004 | Lb/in (min) | 325 |
|  |  | Lb force/in width (min) | 8 |
| Resistance to Soil Burial |  |  |  |
| (a) Break Strength | ASTM D7176 | % change (maximum) | 5 |
| (b) Elongation |  |  | 20 |
| (c) Modulus at 100% |  |  | 20 |
| Low Temperature Impact | ASTM D1790 | (Pass/Fail) | -20 |
| Dimension Stability | ASTM D1204 (212/F/15 min) | % change (maximum) | 3 |
| Water Extraction | ASTM D1239 | % (maximum loss) | 0.15 |
| Volatile Loss | ASTM D1203 | % (maximum) | 0.70 |
| Hydrostatic Resistance | ASTM D751 | psi (minimum) | 100 |

GI 00206.09 Installation.

- Subgrade preparation:

- Remove deleterious materials from surfaces to receive geosynthetics. Deleterious materials include:

- Organic material and particles.

- Particles greater than 3-inches in size.

- Any sharp or jagged rock fragments or materials penetrating the subgrade.

Pavement Subgrade soil shall be prepared as per section C203. PREPARATION OF ROADWAY PAVEMENT SUBGRADE of the City of New Orleans General Specifications for Street Paving and as indicated on the construction drawings or as directed by the project Designer.

Geotextile Installation:

- Install as shown in the Drawings, according to the manufacturer recommendations for anchoring, overlap and other considerations.

Pull material taut and place free of wrinkles.

Field conditions: Unless otherwise noted, overlap geotextile a minimum of 24 inches.

GI 00206.10 Measurement.

- Geosynthetics will be measured in square yards of the type of geosynthetic specified and will be the actual number of square yards complete in place. Costing will need to account for furnishing, transporting, handling, installing, and testing the geosynthetics as well as all seams, overlaps, staking, embedment, and protection measures.

GI 00206.11 Payment.

Payment for geosynthetics will be made at the contract unit prices. Payment will be made under:

| ITEM NO. | PAY ITEM | PAY UNIT |
| --- | --- | --- |
| GI-0206-A-1-N | Geosynthetic (Subsurface Drainage Application, Class 1, Non-woven) | SY |
| GI-0206-A-1-W | Geosynthetic (Subsurface Drainage Application, Class 1, Woven) | SY |
| GI-0206-B-1-N | Geosynthetic (Subsurface Drainage Application, Class 2, Non-woven) | SY |
| GI-0206-B-1-W | Geosynthetic (Subsurface Drainage Application, Class 2, Woven) | SY |
| GI-0206-C | Geosynthetic (Pervious Paving Application) | SY |
| GI-0206-D | Geosynthetic (Impermeable Membrane) | SY |
| GI-0206-E | Geogrid | SY |