# GI 00605

PERVIOUS INTERLOCKING CONCRETE PAVERS

GI 00605.01 Description. The Contractor shall furnish all labor, materials, equipment, and incidentals required and install the concrete paving units as shown on the Drawings and as specified herein.

Pervious interlocking pavers, once installed, shall be protected by the contractor from any placement or contamination of stone infill from soils or other materials which might impact drainage characteristics or staining of pavers from construction vehicles operating on or adjacent to paver areas. After pavers are installed, the contractor shall maintain depth of joint filler stone to top of pavers including additional application of joint filler stone material and compaction over all new pervious paver areas, just prior to project acceptance in order to supplement any visibly settled aggregate materials and resetting of any pavers that have moved out of position or alignment, as directed by the project Designer, and as specified herein.

# GI 00605.02 Applicable Specifications

City of New Orleans Department of Public Works General Specifications for Street Paving (Current Standards)

NO DPW C201:	CLEARING AND GRUBBING

NO DPW C202:	REMOVAL OF STRUCTURES AND OBSTRUCTIONS NO DPW C203:	PREPARATION OF ROADWAY PAVEMENT SUBGRADE NO DPW C204:	ENVIRONMENTAL PROTECTION AND STORMWATER

POLLUTION PREVENTION PLAN

NO DPW C719:	LANDSCAPING

NO DPW C723:	GRANULAR MATERIAL

LA DOTD Standard Specifications For Roads And Bridges (Current Standards)

LA DOTD 203:	EARTHWORK AND SITE PREPARATION, TEMPORARY

EROSION CONTROL

LA DOTD 701:	INCIDENTAL CONSTRUCTION, CULVERTS AND STORM

DRAINS

LA DOTD 702:	INCIDENTAL CONSTRUCTION, MANHOLES, JUNCTION

BOXES, CATCH BASINS, AND END TREATMENTS LA DOTD 711:	INCIDENTAL CONSTRUCTION, RIPRAP

LA DOTD 712:	INCIDENTAL CONSTRUCTION, REVETMENTS

LA DOTD 726:	INCIDENTAL CONSTRUCTION, BEDDING MATERIAL LA DOTD 1018:	MATERIALS, MISCELLANEOUS MATERIALS

LA DOTD 1019:	MATERIALS, GEOTEXTILE FABRIC AND GEOCOMPOSITE SYSTEMS

City of New Orleans Green Infrastructure Specifications (Current Standards)

GI 00126:	SITE ACTIVITY PLAN FOR PROJECTS CONTAINING GREEN INFRASTRUCTURE FACILITIES

GI 00200:	EARTHWORK FOR GREEN INFRASTRUCTURE FACILITIES

GI 00204:	EROSION AND SEDIMENTATION CONTROL GREEN INFRASTRUCTURE FACILITIES

GI 01003:	AGGREGATES FOR GREEN INFRASTRUCTURE FACILITIES

# GI 00605.03 Applicable Standards

- American Society for Testing and Materials (ASTM):

  - C 33	Specification for Concrete Aggregates

  - C 67	Standard Test Methods for Sampling and Testing Brick and Structural Clay Tile

  - C 136	Method for Sieve Analysis for Fine and Coarse Aggregate

  - C 140	Sampling and Testing Concrete Masonry Units

  - C 1701/1701M09	Standard Test method for Infiltration Rate of In Place Pervious 				Concrete

  - C 1781	Standard Test Method for Surface Infiltration Rate of Permeable Unit Pavement 	Systems

  - C 936	Standard Specification for Solid Concrete Interlocking Paving Units

  - C 979	Specification for Pigments for Integrally Colored Concrete

  - D 448	Standard Sizes of Processed Aggregates

  - D 698 & D 1557  Test Methods for Moisture Density Relations of Soil and Soil

Aggregate Mixtures

  - D 2922	Standard Test Method for Density of Soil and Soil-Aggregate In-Place by

Nuclear Methods (shallow depth)

  - D 2940  Graded Aggregate Material for Bases or Sub bases for Highways or Airports

- CSA A231.2-95 – Precast Concrete Pavers

- Interlocking Concrete Pavement Institute (ICPI)

  - Permeable Interlocking Concrete Pavement Manual

GI 00605.04 Submittals. Contractor shall submit to the project Designer:

- A minimum of five sample paving units including manufacturer’s literature, product data, color chart, and samples that indicate color, texture, overall dimension, weight, and shape.

- Pattern layout and details of construction and accessories required.

- Test results from an independent testing laboratory for compliance of paving unit requirements to ASTM C 936 and CSA A231.2-95 for resistance to freeze thaw and other applicable requirements.

- Sieve analysis for grading of bedding, aperture, and joint aggregates and materials.

# GI 00605.05 Quality Assurance

- Paver manufacturer shall be an Interlocking Concrete Paver Institute (ICPI) Certified Producer

- Installation shall be performed by a contractor with at least 5 years of experience in placing interlocking concrete pavers on projects of similar size and scope.

- Contractor shall have received training by a certified instructor for the ICPI (Interlocking Concrete Paver Institute) Contractor Certification Program.

- Visual Inspection:

  - All units shall be sound and free of defects that would interfere with the proper placing of the unit or impair the strength or permanence of the construction. Surface cracks incidental to the usual methods of manufacture, or surface chipping resulting from customary methods of handling in shipment and delivery, shall not be deemed grounds for rejection.

  - Cracks exceeding 0.25 inches in width and/or 1.0 inch in depth shall be deemed grounds for rejection.

  - Blocks rejected prior to delivery from the point of manufacture shall be replaced at the manufacturer's expense. Blocks rejected at the job site shall be replaced at the expense of the contractor.

- Field Demonstration

  - Prior to starting the work, a 10-ft x 10-ft area shall be installed to determine setting bed, joint sizes, lines, laying pattern, edging interface, and the color and texture of the pavers to be used on the project.

  - The approved mock-up will be the standard by which the work shall be judged and shall be left undisturbed until the work is completed. The approved mock-up may be incorporated into the work.

- Acceptance

  - Infiltration Performance: The Pervious Pavers will only be accepted when accompanied by documented third party surface infiltration performance characteristics based on ASTM C1701/C1701M-09 or C1781. The surface infiltration rate shall be no less than 300 inches per hour on an outdoor working surface, with typical base material utilized for the test.

  - Structural Performance for Vehicular Traffic Areas:

    - Traffic Rated (Vehicular): The design of the Pervious Pavers shall be capable of supporting AASHTO HS-20, H-20 and HS-25 truck loading. The blocks should be analyzed as unreinforced supporting a uniform truck tire load with impact per AASHTO standards. As with all vehicular traffic paving systems, the subgrade soil, geosynthetic and base preparation for the Pervious Pavers must be properly designed and prepared. This is critical to the performance of the system.

# GI 00605.05 Delivery, Storage, and Handling

- Comply with manufacturer’s instructions and lead-time requirements to avoid construction delays.

- Protect concrete pavers and accessory materials during shipment, storage and construction against staining and damage.

- Coordinate delivery and paving schedule to minimize interference with other construction activity.

- Cover sands with waterproof covering to prevent exposure to rainfall or removal by wind. Do not install sand or pavers during heavy rain or snowfall, or over frozen base materials. Do not install bedding layers over frozen base materials.

# GI 00605.06 Materials

- Permeable Concrete Pavers, Vehicular:

    - The interlocking paving units shall conform to reference standard ASTM C 936. The units shall have a 28-day compressive strength minimum of 8,000 psi with no individual unit less than 7,200 psi. No paver shall have a water absorption of greater than 5% when tested in accordance with reference standard ASTM C140.

    - Pavers shall have freeze thaw resistance according to reference standard ASTM C67 Section 8.

    - All pavers shall be by the same manufacturer.

    - Size, shape, design and colors shall be in accordance with the Drawings and specifications and shall match samples approved by the project Designer.

    - Paving unit shall have interlocking joints with a minimum of two vertically aligned horizontal interlocking spacer bars on each of its sides exhibiting unit to unit horizontal restriction movement in both horizontal axes.

    - Paving Unit Chamfer: Paving unit shall have a maximum 1/16 in. (1.5 mm) chamfer to minimize vibration in the wheeled traffic traveling the jointed surface.

- Permeable Concrete Pavers, Pedestrian:

  - The paver requirements described in 00206.07 (a) may be used for pedestrian applications or the project designer may specify pedestrian only pavers. Details for pedestrian only pavers will be provided by the project designer as part of the contract documents.

  - Paver joint width shall be a nominal 1/4 in. (7 mm) installation width to comply with being less than the ADA maximum horizontal surface open area.

- Aggregate Fill: Bedding course, filter/bridging aggregate, storage aggregate, and joint filler material shall be as specified in GI 01003.

- Filter fabric shall be non-woven and in accordance with GI 00206.

# GI 00605.07 Installation

- General

  - Any excess thickness of soil applied over the excavated soil subgrade to trap sediment from adjacent construction activities shall be removed before application of the Geotextile and subbase materials.

  - Keep area where pavement is to be constructed free from sediment during entire job. Geotextiles base and bedding materials contaminated with sediment shall be removed and replaced with clean materials.

  - Do not damage drainpipes, overflow pipes, observation wells, or any inlets and other drainage appurtenances during installation. Report any damage immediately to the Project Engineer.

  - Remove and dispose of all organic and unsuitable material from subgrade soil. Subgrade soil shall be graded uniform and parallel to finished grade and, if deemed by the project designer, compacted to 95% of maximum dry density in accordance with ASTM D-1557.

  - Compaction shall not be less than 95% Standard Proctor Density in accordance with ASTM D 698 for areas subject to pedestrian traffic only. All pavement subject to vehicular traffic shall be compacted to not less than 95% Modified Proctor density according to ASTM D 1557.

- Geotextiles

- Place per Plan detail. Secure in place to prevent wrinkling from vehicle tires and tracks.

- Overlap a minimum of 12 in. in the direction of drainage.

- Open-graded subbase and base (Storage and Filter)

- Moisten, spread, and compact the subbase in lifts without wrinkling or folding the geotextile. Place subbase to protect geotextile from wrinkling under equipment tires and tracks.

- The storage course shall be placed in layers uniformly spread and compacted. For vehicular areas, the material shall be placed in 4-in to 6-in thick lifts and compacted using a plate rammer or vibratory roller. Base material for pedestrian areas may be placed in 4-in thick lifts and compacted using a plate compactor capable of exerting no less than a 5000-lb force.

- In areas not accessible by rolling equipment, compact to specified density with hand operated equipment.

- For each lift, make at least two passes in the vibratory mode then at least two in the static mode with a vibratory roller (10T minimum) until there is no visible movement of the stone. Do not crush aggregate with the roller.

- The surface tolerance of the compacted subbase shall be ± ¾ in. over a 10 ft straightedge.

- Moisten, spread, and compact the Filter layer in one thick lift. On this layer, make at least two passes in the vibratory mode then at least two in the static mode with a vibratory roller (10T minimum) until there is no visible movement of the stone. Do not crush aggregate with the roller.

- The surface tolerance of compacted base should not deviate more than. ±1/2 in. over a 10 ft straightedge.

- Bedding layer

- Vehicular:

  - Moisten, spread, and compact the bedding material. Compact with a minimum 10 T static roller. Make at least 4 passes. No visible movement should occur in the base material when compaction is complete. Do not crush aggregate with the roller.

  - The surface tolerance of the compacted surface should not deviate more than ±½ in. over a 10 ft. straightedge.

  - Do not subject bedding material to any pedestrian or vehicular traffic before paving unit installation begins.

- Pedestrian:

  - Moisten, spread, and screed the stone bedding material.

  - Fill voids left by removed screed rails with stone.

  - The surface tolerance of the screeded bedding layer shall be ±3/8 in over a 10 ft straightedge.

  - Do not subject screeded bedding material to any pedestrian traffic before paving unit installation begins.

- Permeable interlocking concrete pavers and joint/opening fill material

- Lay the paving units in the pattern(s) with nominal joint widths. Maintain straight pattern lines.

- Fill gaps at the edges of the paved area with cut units. Cut pavers subject to tire traffic shall be no smaller than 1/3 of a whole unit.

- Cut pavers and place along the edges.

- Fill the openings and joints with stone.

- Remove excess aggregate on the surface by sweeping pavers clean.

- Compact and seat the pavers into the bedding material using a low-amplitude, 75-90 Hz plate compactor capable of at least 5,000 lbf (22 kN) centrifugal compaction force. This will require at least two passes with the plate compactor.

- Do not compact within 6 ft of the unrestrained edges of the paving units.

- Apply additional aggregate to the openings and joints if needed, filling them completely. Remove excess aggregate by sweeping then compact the pavers. This will require at least two passes with the plate compactor.

- All pavers within 6 ft of the laying face must be left fully compacted at the completion of each day.

- The final surface tolerance of compacted pavers shall not deviate more than ±3/8 in. under a 10 ft long straightedge.

- The surface elevation of pavers shall be 1/8 to 1/4 in. above adjacent drainage inlets, concrete collars, or channels.

# GI 00605.08 Maintenance.

- Pervious pavement installation shall maintain a minimum infiltration rate of 200 inches per hour and infiltration testing shall be performed by contractor in accordance with ASTM C1701 or C1781 prior to substantial completion.

- Paver joints shall be filled with joint filler stone at least three times after installation or on a monthly basis until project acceptance.

- Extra Materials: Contractor to provide 10 sq ft of additional material per pervious installation for the owner to use for maintenance and repair. Pavers shall be from the same production run as installed.

- The manufacturer or representative of the Pervious Paver shall provide a minimum 36- month maintenance program, including a visual inspection report with photos and a recommended cleaning schedule. Maintenance of the Pervious Paver shall effectively restore infiltration to a minimum of 90+% performance of design and be tested per ASTM C1701 or C1781.

# GI 00605.09 Measurement.

- Pervious pavers will be measured in square feet for the type(s) specified in the Contract Documents. The actual number of square feet completed in place will be paid for at the contract unit price which will include unit pavers, bedding course, and joint filler. Payment will also include costs for furnishing all materials, labor, tools, equipment, and incidentals to complete the work, including the 36-month maintenance program.

GI 00605.11 Payment. Payment for pervious pavers will be made at the contract unit prices. Payment will be made under:

| ITEM NO. | PAY ITEM | PAY UNIT |
| --- | --- | --- |
| GI 0605-01-A | Pervious Interlocking Concrete Pavers, Vehicular (size) | Square Foot |
| GI 0605-02-B | Pervious Interlocking Concrete Pavers, Pedestrian (size) | Square Foot |