# GI 00606

PRECAST POROUS CONCRETE PANEL

GI 00606.01 Description. The Contractor shall furnish all labor, materials, equipment, and incidentals required and install the precast porous concrete panels as shown on the Drawings and as specified herein.

This section describes the installation of the precast porous concrete panels (PPCP). The purpose of the precast porous concrete panel is to provide the structural support of conventional pavement and to serve as a porous medium for infiltration of stormwater runoff through its surface.

# GI 00606.02 Applicable Specifications

City of New Orleans Department of Public Works General Specifications for Street Paving (Current Standards)

NO DPW C201:	CLEARING AND GRUBBING

NO DPW C202:	REMOVAL OF STRUCTURES AND OBSTRUCTIONS NO DPW C203:	PREPARATION OF ROADWAY PAVEMENT SUBGRADE NO DPW C204:	ENVIRONMENTAL PROTECTION AND STORMWATER

POLLUTION PREVENTION PLAN

NO DPW C707:		  CURBS AND GUTTERS

NO DPW C719:	LANDSCAPING

NO DPW C723:	GRANULAR MATERIAL

LA DOTD Standard Specifications For Roads And Bridges (Current Standards)

LA DOTD 203:	EARTHWORK AND SITE PREPARATION, TEMPORARY

EROSION CONTROL

LA DOTD 701:	INCIDENTAL CONSTRUCTION, CULVERTS AND STORM

DRAINS

LA DOTD 702:	INCIDENTAL CONSTRUCTION, MANHOLES, JUNCTION

BOXES, CATCH BASINS, AND END TREATMENTS LA DOTD 711:	INCIDENTAL CONSTRUCTION, RIPRAP

LA DOTD 712:	INCIDENTAL CONSTRUCTION, REVETMENTS

LA DOTD 726:	INCIDENTAL CONSTRUCTION, BEDDING MATERIAL LA DOTD 1018:	MATERIALS, MISCELLANEOUS MATERIALS

LA DOTD 1019:	MATERIALS, GEOTEXTILE FABRIC AND GEOCOMPOSITE SYSTEMS

City of New Orleans Green Infrastructure Specifications (Current Standards)

GI 00126:	SITE ACTIVITY PLAN FOR PROJECTS CONTAINING GREEN INFRASTRUCTURE FACILITIES

GI 00200:	EARTHWORK FOR GREEN INFRASTRUCTURE FACILITIES

GI 00204:	EROSION AND SEDIMENTATION CONTROL GREEN INFRASTRUCTURE FACILITIES

GI 00206:	GEOSYNTHETICS FOR GREEN INFRASTRUCTURE FACILITIES

GI 01003:	AGGREGATES FOR GREEN INFRASTRUCTURE FACILITIES

# GI 00606.03 Applicable Standards

- American Society for Testing and Materials (ASTM):

  - C 33	Specification for Concrete Aggregates

  - C 136	Method for Sieve Analysis for Fine and Coarse Aggregate

  - C 42	Standard Test Method for Obtaining and Testing Drilled Cores and Sawed 	Beams of Concrete

  - C 78       Standard Test Method for Flexural Strength of Concrete (Using Simple 		        Beam with Third-Point Loading)

  - C 136	Standard Test Method for Sieve Analysis of Fine and Coarse Aggregates

  - C 1116	Standard Specification for Fiber-Reinforced Concrete

  - C 1688	Standard Test Method for Density and Void Content of Freshly Mixed Pervious 	Concrete

  - C 1701/1701M09	Standard Test method for Infiltration Rate of In Place Pervious 				Concrete

  - D 698 & D 1557  Test Methods for Moisture Density Relations of Soil and Soil

Aggregate Mixtures

  - D 1751   Standard Speciﬁcation for Preformed Expansion Joint Filler for Concrete 		        Paving and Structural Construction (Non-extruding and Resilient Bituminous   	        Types)

GI 00606.04 Submittals.

- All materials requiring a submittal for review and approval must be submitted by the Contractor to project Designer prior to purchase of those materials.

- Shop drawings that must be submitted prior to pre-construction meeting include:

  - Installation plan showing layout of each precast porous concrete panel with identification mark intended for installation.

  - Individual slab drawings detailing lifting points in surface, reinforcing, finishes, and all dimensions.

  - Narrative of shipping, handling, and protection procedures.

- Test results performed by an independent AASHTO Materials Reference Laboratory (AMRL) accredited testing laboratory of the following:

  - Density and void content results in accordance with ASTM C1688 Standard Test Method for Density and Void Content of Freshly Mixed Pervious Concrete, and

  - Flexural strength test results in accordance with ASTM C78 Flexural Strength of Concrete. Three (3) saw-cut concrete beams prepared specifically for testing purposes as per ASTM C78, with the same concrete mix and reinforcing characteristics would be representative of a full-size panel. Changes in reinforcement configuration for testing purposes will not be permitted. The Contractor must submit a drawing for approval of the concrete beams intended for testing with all the reinforcing and lifting hook placements indicated. No end caps on the beams intended for testing will be permitted. One percent (1%) of the total number of panels intended for the entire project will be tested for compliance with the specifications.

  - Infiltration rate of Precast Porous Concrete Paving Panels in accordance with ASTM C1701 Standard Test Method for Infiltration Rate of In-Place Pervious Concrete. One percent (1%) of the total number of panels intended for the entire project will be tested for compliance with the specifications.

- Particle size analysis in accordance with ASTM C136 with approved source(s) of supply noted.

- Test method procedures to conduct percolation rate testing after installation in accordance with ASTM C1701 Test Method for Infiltration Rate of In-Place Pervious Concrete. The submittal must include information related to the testing apparatus being used (infiltration rings) for approval by the City.

# GI 00606.05 Quality Assurance

Quality Assurance Plan must be furnished by the Contractor and must receive approval from the Designer at least five (5) working days prior to commencing any work.

The plan must include, but is not limited to, horizontal and vertical layout of the work, methods for the installation of the edge restraints, the methods for placing of the subbase aggregate and the placing of the panels.

A review of the Contractor’s Quality Assurance installation plan will be done at a pre-construction meeting with the Contractor, the Contractor’s panel installer mechanic/subcontractor, the panel manufacturer’s representative (if present on the site), the Designer.

The installation Contractor must be responsible for reviewing and complying with the Manufacturer’s installation requirements including any required trainings, if applicable. The Contractor will be responsible for reviewing and abiding by the Manufacturer’s Handling and Installation instructions.

# GI 00606.06 Delivery, Storage, and Handling

# Delivery of the precast porous concrete panels must be coordinated so as not to interfere with other construction in the project to avoid delays.

# Precast porous concrete panels must be handled per Manufacturer recommendations which were included in the approved submittal.

# Offloading of panels must be performed by trained and experienced equipment operators. Extra care must be taken while offloading the panels due to their unique structural characteristics. A forklift or similar machine with forks must be used to offload. Chains, cables, or slings must not be wrapped around slabs and only the lifting points must be utilized.

# Precast porous concrete panels must be visually inspected for completeness, texture, and consistency with the approved shop drawings and the installation drawings. Minor spalls and cracks will be the basis for rejection. Defective panels will be inspected by the Designer and the decision will be made at his/her sole discretion.

# Panels must be stored such that they are kept free from mud, dirt, grass cuttings, accumulation of foliage and debris at all times.

# Panels must not be exposed unsecured to vehicular and pedestrian traffic. Skid steer and forklift equipment must be kept off unsecured paving panels.

# Geogrid, geofabrics, aggregate, and liner materials must be kept clean and prepared for installation.

# Stored panels must be placed on a level or nearly level paved surface. In dusty environment, panels must be covered to prevent dust and debris from settling on panel surfaces.

# GI 00606.07 Materials

- Precast Porous Concrete Panel

- The precast porous concrete panels must be supplied by a manufacturer having at least five (5) years of experience in the production and sale of porous concrete panels.

- The manufacturer must provide a training program for the Contractor detailing handling and installation of the product.

Concrete average unit weight must be 120 lb./ft.3 (+/- 4%). The average core compressive strength of the precast porous concrete panels must be a minimum of 2,000 psi at 28 days per ASTM C42. The manufacturer must cure the precast porous concrete panels. The precast porous concrete panels must have a minimum infiltration rate of 200 inch/hr when tested in accordance with ASTM C1701.

- Refer to Contract Drawings for precast porous concrete panel dimensions, thickness, and reinforcing requirements. The precast porous concrete panels supplied must be of the type(s) as shown in the Contract Drawings.

- Precast porous concrete panels shall be reinforced with ultra-thin monofilament homopolymer polypropylene fibers equivalent to MasterFiber 100 manufactured by BASF Corporation or approved equal.

- Minor adjustments of the limits of work will be considered by the Designer to reduce the number of panels less than full length to eliminate cutting. Smaller lengths must only be used where necessary and appropriate to accommodate utilities and overall alignment or as shown on the Contract Drawings.

- Installation of precast porous concrete panels must be in strict accordance with the manufacturer’s recommendations, all information contained in this specification, and related contract drawings.

- Permanent lifting points must be embedded in the panel surface for unloading, handling, installation, maintenance, removal, and reinstallation purposes. Refer to Contract Drawings for lifting point locations. Shop drawings are required. All panels must be provided with lifting point protection caps and approved lifting swivels for use in covering the embedded lifting points. Any altered unit must include a minimum of two (2) permanent lifting points.

- Precast porous concrete panels must have a minimum average Flexural Strength of 400 psi when tested in accordance with ASTM C78. Panels must not be shipped until they have achieved 85% of the minimum flexural strength or higher as determined by the lab test results submitted. The void content must be from 15% to 25%, conforming to ASTM C1688 or ASTM D1754/1754M-12.

- Each individual precast porous concrete panel must be weighed, and the unit must be labelled with the weight, size, and date of manufacture.

- All panels must be provided with spacers preventing slab to slab contact, as required by the Manufacturer.

# GI 00606.08 Installation

- General

  - Before panels are installed, the Contractor must ensure that all materials and preparation for subbase and edge restraints are installed in accordance with Contract Drawings and specifications and accepted by the Designer.

  - Do not damage drainpipes, underdrains, cleanouts, roadway boxes, manholes, or any other utilities during installation. Report any damage immediately to the Designer. All damage must be replaced or repaired as part of the bid price of this item by the Contractor at no additional cost to the city.

- Subgrade Preparation

  - The subgrade under the storage aggregate layer must not be compacted.

  - Prepared subgrades under all infiltration areas must not be compacted and must not be subjected to construction equipment traffic. Where erosion has caused accumulation of sediment or ponding on the subgrade, remove sediment with light equipment and/or manually. Scarify the underlying soils to a minimum depth of six-inches (6”) with a York-type rake or equivalent equipment to the satisfaction of the Designer.

  - Restore any subgrade areas damaged by erosion, ponding, or traffic compaction to design line and grades prior to installation of geogrid and storage aggregate layer.

  - Any excess thickness of material placed over the soil subgrade to trap sediment transported by runoff from adjacent construction areas must be removed before placement of geogrid and storage reservoir layer. Keep area where precast porous concrete panels are to be installed free of sediment during the entire construction period. Any materials that are contaminated with sediment must be removed and replaced with clean materials.

- Concrete Edge Restraint

Concrete edge restraint must comply with contract drawings and typical details and must be placed prior to the placement of the geogrid or storage aggregate layer.

- Concrete Curb

Concrete curbs must comply with DPW Specifications Section C707.

- Non-Woven Geotextile Fabric

Non-woven Geotextile Fabric must comply with GI 00206.

- Geogrid

Geogrid must comply with DPW Specification Section C203.

- Waterproof Membrane

Waterproof membrane must comply with GI 00206.

- Storage Aggregate Layer

  - Storage aggregate layer must comply with GI 01003.

  - Storage aggregate layer must be compacted to at least 95% Modified Proctor relative compaction per ASTM D1557. A minimum 200-pound walk- behind plate compactor must be used on each lift of maximum 10”. Compaction using the plate compactor must include four (4) passes in each direction longitudinally along length of the trench.

  - The surface tolerance of the compacted storage aggregate layer must be a maximum of +/- three-quarter inch (¾") under a ten (10) foot straightedge in all directions.

  - Verify that the storage aggregate layer, as shown on the Contract Drawings, has been properly placed within the trench and compacted as approved and accepted by the Designer before the bedding course is placed.

  - Place and spread bedding course stone evenly over screed rails to achieve a thickness of two inches (2”) minimum. Level the surface of bedding course stone with a screed, it must not be compacted.

  - The surface tolerance of the screed bedding course must be a maximum of a +/- one-quarter inch (¼") under a ten (10) foot straightedge in all directions. The cost of any additional stone beyond the limits must be borne by the Contractor at no additional cost to the city.

  - Once installed, Contractor must not disturb screeded bedding course.

- Precast Porous Concrete Panel Placement

- Precast porous concrete panels must not be placed on a saturated or frozen base.

- Precast porous concrete panels must only be lifted and placed using swivels and spreader chains. Chains, cables, or slings should never be wrapped around the panel for lifting under any circumstances. Swivels must be securely bolted snug but not over-tightened to avoid damage to the surface of the panel.

- Contractor must keep skid steer, forklift, and all other heavy equipment off all unrestrained panels.

- Lay panels in pattern(s) shown on approved shop drawings layout plan. Cut panels to complete installed length and pattern on approved shop drawings.

- Contractor is responsible for installing precast porous concrete panels according to the Manufacturer’s requirements for proper handling and installation.

- To prevent any damage to panel edges, Contractor must place panels with the joint size specified without using metal hammers, pry bars or drift pins. Horizontal adjustments to the placement of laid slabs must be made with wood wedges and levers, and rubber mallets as needed. Joint widths and lines must be continually evaluated and straightened as necessary as paving proceeds to the satisfaction of the Designer.

- Panels must be placed parallel to the adjacent edge restraint as per approved shop drawings. Any adjustments must be made at the curb for irregular alignment.

- Unless otherwise directed, adjacent slabs must be separated from each other by one-eighth inch (1/8”) to provide open joints between panel slabs of one- eighth inch (1/8”) wide using spacers provided by the manufacturer of the panels to ensure proper joint spacing. No joints must exceed one-eighth inch (1/8”) in width unless otherwise directed by the Designer in writing.

- Panel to panel joints must be left open. No stone or sand is to be placed in joints.

- Horizontal joint lines along header must not deviate more than ± one-half inch (½") over 50 feet from reference string lines.

- The precast porous concrete panels must be installed so that there is no lippage or surface unevenness greater than one-eighth inch (1/8”) difference in height between panels and adjacent surfaces.

- Contractor must complete any gaps at the edges of the paved area with panels cut according to manufacturer’s requirements for minimum panel dimensions. Cut panels to meet installation dimensions as indicated on the approved panel layout shop drawings. End panels to be placed along the edge or corners must be cut with a masonry saw. Cut units must be no shorter than one-quarter (1/4) of a whole panel length and must still retain the minimum number of lifting points required.

- Contractor must protect adjacent panels’ surfaces from dust or debris infiltration when cutting panels.

- Contractor must finish outside edge joints as indicated on the approved installation plan with approved joint filler material.

- After an area is completely paved, Contractor must complete a final setting of the precast porous concrete panels into the screed leveling course layer by trafficking with light-weight rubber-tired equipment approved by the Designer.

- Contractor must remove and replace any panels cracked or damaged during installation with equivalent replacement panels. Contractor must all reset panels not in conformance with specified installation tolerances to the satisfaction of the Designer.

  - Hairline cracks (1/8” or smaller) with no vertical or horizontal displacement of panels shall be considered as to not interfere with the proper functioning or performance of the system and are acceptable when immediately repaired upon observation per manufacturers recommendation. Where approved by the Designer, larger cracks (1/8” or larger) with no vertical displacement may be repaired under the direction of the manufacturer. Any cracked panels with horizontal displacement of greater than 1/4" or a vertical displacement of any size shall be replaced.

  - The repairs must be properly finished and cured. The color of the repair area must match as closely as possible with the rest of the panel color. Repairs shall be made with a mixture of self-leveling polyurethane sealant for horizontal applications and cement, as directed by the manufacturer.

- Contractor must warranty from the date of install to substantial completion that all installed panels are free of rocking or pumping as evidenced by visible vertical movement. Any panels observed to be moving or displacing must be removed, the screeding leveling course re-screeded, and the panels reset and/or replaced if cracked.

- Contractor must verify and report to the Designer in writing that the final surface elevations of the set panels are in conformance with the Contract Drawings. The final surface tolerance from grade elevations must not deviate more than ± one-eighth inch (1/8”) under a ten-foot (10’) straightedge.

- The surface elevation of set panels must be flush with all manholes and the top of utility structures.

- Protection

  - Immediately after precast porous concrete panels have been placed, insert plastic caps in lifter holes as provided.

  - After work in this section is complete, the Contractor will be responsible for protecting the precast porous concrete panel system from damage and/or contamination during the remainder of work on site. The surface of the precast porous concrete panels must be completely covered during the placement of adjacent soils or paving materials in a manner approved by the Designer.

- Acceptance

  - Prior to acceptance by the City for Substantial Completion, the Contractor must conduct percolation rate testing every hundred (100) linear feet of gutter but no less than three (3) per section of gutter in accordance with ASTM C1701. All testing must be done in coordination with and in the presence of the Designer.

  - Testing locations will be chosen at the Designer’s discretion and in accordance with the ASTM requirements.

  - Contractor must provide testing results to the City within seven (7) days after the completion of testing. The Contractor must review testing results with the City. Precast porous concrete panels with infiltration rates below the minimum infiltration rate of 200 inches per hour prior to Substantial Completion must undergo corrective action (such as cleaning the failed panel, or cleaning the entire gutter run, or cleaning/replacing the subbase aggregate, or replacement of the failed panel) prior to the City issuing Substantial Completion.

  - After corrective action has taken place, then one other panel in the same contiguous length of porous gutter will be randomly selected by the Designer and tested to ensure that the gutter meets the specified infiltration rate. If the selected panel fails to meet that rate, then the whole length of the installation must be cleaned again, and the testing process repeated until passing results are obtained.

# GI 00606.09 Maintenance.

- Infiltration rate testing, in lieu of cleaning and maintenance, during the guarantee period will not be acceptable.

The Contractor must conduct periodic maintenance and cleaning for the duration of the guarantee period after substantial completion, at minimum, as described below:

- May or June

- December or January

- Just prior to end of the guarantee period, unless the porous concrete panels were last cleaned within 120 calendar days.

- Procedures for Maintenance and Cleaning:

- The Contractor must remove all visible sediment deposits. Where sediment has accumulated in areas surrounding and/or upstream of the precast porous concrete panel system and may enter the porous concrete, the Contractor must also remove such visible sediment deposits.

- The Contractor must use vacuum cleaning, regenerative air machines equipped with a specialized vacuum head that includes high pressure water nozzles. Walk behind and handheld equipment are not acceptable for use. This maintenance must remove sediment and debris that has clogged or blocked voids in the precast porous concrete panel.

- Sediment and debris must be sufficiently removed after cleaning to allow the porous pavement to infiltrate stormwater runoff. This may require multiple passes of cleaning to meet the desired post-cleaning infiltration rate, as discussed below.

- After cleaning of the precast porous concrete panel system and no later than three calendar (3) days after cleaning, the Contractor must conduct percolation rate testing every hundred (100) linear feet of the installation but no less than two (2) per section of installation in accordance with ASTM C1701. All testing must be done in coordination with and in the presence of the Designer.

- Testing locations will be chosen at the Designer’s discretion and in accordance with the ASTM requirements.

- The Contractor must provide testing results to the City within seven (7) days after the completion of testing. The Contractor must review testing results with the City. Precast porous concrete panels with infiltration rates below the minimum infiltration rate of 150 inches per hour specified must undergo corrective action (such as further cleaning or replacement).

- After corrective action has taken place, then one other panel in the same contiguous length of porous gutter will be randomly selected by the Designer and tested to ensure that the gutter meets the specified infiltration rate. If the selected panel fails to meet that rate, then the whole length of the gutter must be cleaned again, and the testing process repeated until passing results are obtained.

- Cleaning will be deemed sufficient only if the minimum of 150 inch/hr infiltration rate required by the city has been met. The City will conduct field inspections to ensure the proper condition and performance of the precast porous concrete paving panel system. Visual inspections and infiltration tests will be used to determine the performance of porous concrete. If based on visual inspections and/or the test results reviewed by the Designer, the City determines that the Contractor’s performance of maintenance work is insufficient, the Contractor will submit a revised method or schedule for the maintenance of precast porous concrete paving panels. The Contractor must perform subsequent corrective maintenance work at no additional cost to the City.

- The Contractor must responsibly decant dirty water in accordance with LDEQ regulations.

- The equipment information, operating procedures including disposal, and schedule for maintenance work must be submitted to the City at least 45 calendar days prior to start of maintenance and cleaning. Maintenance and cleaning cannot begin until approved by the Designer.

# GI 00606.10 Measurement.

- Precast porous concrete panels will be measured in square feet for the type(s) specified in the Contract Documents. The actual number of square feet completed in place will be paid for at the contract unit price which will include unit pavers, bedding course, and joint filler. Payment will also include costs for furnishing all materials, labor, tools, equipment, and incidentals to complete the work, including the 36-month maintenance program.

GI 00606.11 Payment.

Payment for precast porous concrete panels will be made at the contract unit prices. Payment will be made under:

| ITEM NO. | PAY ITEM | PAY UNIT |
| --- | --- | --- |
| GI 0606-01 | Precast Porous Concrete Panel | Square Yard |