GI 01003

AGGREGATES

FOR GREEN INFRASTRUCTURE FACILITIES

- GI 01003.01 Description.

- This work shall include, but not be limited to, the installation of all aggregates shown on the Drawings and specified herein. This Special Provision is intended to be a complement to technical specifications provided by the project Engineer or Landscape Architect.

GI 01003.02 Applicable Standards

- Contractor to comply with all applicable requirements of the City of New Orleans Department of Public Works typical roadway sections for street construction, as issued by the City of New Orleans DPW.

GI 01003.03 Submittals. Contractor shall submit to the Engineer/Landscape Architect the following information:

- Samples for each bulk-supplied material in sealed containers labeled with content, source, and date obtained. Sample shall include the following information:

- Material source certifications.

- Cleanliness certification that aggregate is double-washed.

- Properties certifications for each aggregate type.

GI 01003.04 Quality Assurance.

- Contractor shall obtain an independent testing agency to sample and test the aggregate for the following:

- Gradation – test each sample of aggregate for gradation in accordance with ASTM C136.

- Contractor shall comply with aggregates from Table 1 in accordance with ASTM D448-03a.

  - The maximum size of the filter/bridging course aggregate should be the smallest size of the storage aggregate layer to prevent mixing of materials.

GI 01003.05 Materials.

- Aggregate materials shall be graded crushed stone or gravel, angular in shape, and free from all organic materials and debris. Aggregates shall be double-washed and cleaned from all fines or other deleterious materials before being delivered to the construction site.

- Bedding (Leveling) Course:

- Depth: 1 - 2 inches; refer to Drawings

- Size: No. 8, No. 89, or No. 9 aggregate

- Compaction: varies by application.

- Filter/Bridging Course: an aggregate material which functions to prevent Bioretention Media from migrating into courser aggregate below.

  - Depth: 3 inch minimum; refer to Drawings

  - Size: No. 57 or No. 8, note that aggregate size may vary depending on particle size of Bioretention Media above and Storage Aggregate Course below.

  - Compaction: minimum 95% standard proctor, unless otherwise noted to meet minimum infiltration rates.

- Storage Aggregate Course:

  - Depth: 6 inch minimum, varies depending on storage needed; refer to Drawings

  - Size: No. 2 or No. 57, varies by application; refer to drawings. Aggregate size may vary depending on the specified size of the filter/bridging course.

  - Compaction: minimum 95% standard proctor, unless otherwise noted to meet minimum infiltration rates.

- Rip Rap:

  - Depth: varies, refer to Drawings. The minimum thickness of a rip rap layer shall be no less than the spherical diameter of the max stone size in the rip rap class.

  - Size (see LADOTD Table 711-1):

    - Class A – 2 lb stone

    - Class B – 10 lb stone

  - Compaction: n/a

- Joint Filler Stone:

  - Depth: N/A

  - Size: No. 8, No. 89, or No. 9

  - Compaction: N/A

GI 01003.06 Execution.

- Excavate subgrade to depths shown on the Drawings. Engineer/Landscape Architect shall review and approve of subgrade prior to the installation of geotextiles and aggregates.

- Install non-woven geotextile fabric and pipes immediately after the subgrade has been approved.

- Evenly spread aggregate on prepared subgrade and geotextile in thicknesses shown on Drawings. If required, compact aggregate layers in lifts as recommended by geotechnical engineer until desired compaction is reached.

- Do not install aggregate during weather conditions that will have detrimental effects on the quality of the installation.

GI 01003.07 Protection during Suspension of Operations.

- At the conclusion of each day’s work, Contractor shall cover the aggregate with geotextile fabric or impermeable liner to protect from sedimentation washout. Protection shall remain in place until all bare soils are stabilized and vegetated.

GI 01003.08 Measurement.

- Filter/Bridging Aggregate Course will be measured by the Cubic Yard (Net Section) (CY). The length, width, and depth will be measured to the points established by the Drawings. Payment will also include costs for furnished all materials, labor, tools, equipment, and incidentals to complete the work. The measurement will encompass all labor and materials to install and maintain.

- Storage Aggregate Course will be measured by the Cubic Yard (Net Section) (CY). The length, width, and depth will be measured to the points established by the Drawings. Payment will also include costs for furnished all materials, labor, tools, equipment, and incidentals to complete the work. This measurement will encompass all labor and materials to install and maintain.

- Rip Rap will be measured by the Square Yard (SY). The length and width will be measured to the points established by the Drawings. Payment will also include costs for furnished all materials, labor, tools, equipment, and incidentals to complete the work. This measurement will encompass all labor and materials to install and maintain.

SP 01003.08 Payment. Payment for aggregates will be made at the contract unit prices. Payment will be made under:

ITEM NO. 	PAY ITEM PAY 	UNIT

GI 1003-03	Rip Rap	Square Yard

GI 1003-03-A	Rip Rap, Splash Pad (Class A)	Square Yard

GI 1003-04	Bedding Course, (Aggr. size)	Cubic Yard

GI 1003-05	Filter Aggregate, (Aggr. size)	Cubic Yard

GI 1003-06	Storage Aggregate, (Aggr. size)	Cubic Yard